## Slide 1
二维卤素钙钛矿ns2孤对电子效应
对光物理性质的影响探究
谷家桢
导师：傅永平 助理教授
2023.09.16

## Slide 2
Contents
Part. 1 Introduction
Part. 2 Current Progress
- LPE tuning structural distortions
- LPE tuning PLQY
- LPE tuning exciton diffusivity
Part. 3 Future Plan
- Enhancing LPE in other systems
- LPE tuning exciton diffusivity
- LPE tuning excited-state properties

## Slide 3: 1.1 Why 2D Halide Perovskite?
aaa
Inorganic Semiconductors:
- Rigid;
- Static;
- Harmonic lattice;
Hybrid Halide Perovskites:
- Soft;
- Dynamic;
- Strong anharmonicity;
Si
SiC
GaAs
New Properties of Anharmonic SCs?
Well-Studied
3D Perovskite
2D Perovskite

## Slide 4: 1.2 2D Halide Perovskites
Formula
(LA)2(A)n-1BnX3n+1
for n=1:
(LA)2BX4 (B2+ = Pb2+, Sn2+, Ge2+...)
Crystal Structure
"Slicing 3D perovskite ABX3 lattice"
Various LA ==> Great tunability
Heterogeneity ==> Nano-devices
Layered structure ==> Excitonic nature
Nat. Rev. Chem. 2021, 5, 838. Angew. Chem. Int. Ed. 2017, 56, 4252. ACS Nano 2022, 16, 2, 3221. J. Mater. Chem. C, 2018, 6, 12714
Ferroelectrics
Nanoelectronics
Light-emitters
Notes: title explain

## Slide 5: 1.3 ns2 Lone Pair Effect (LPE)
Second-order Jahn-Teller (SOJT) Effect
.
Nat. Rev. Chem. 2021, 5, 838. JACS, 2016, 138, 11820.
ns2 lone pair effect &
off-center displacement
Notes: focus on excited state potential surface & properties
remove t2g right

## Slide 6: 1.3 ns2 Lone Pair Effect (LPE)
Lattice Anharmonicity
Harmonic oscillator:
(Parabola)
With ns2 LPE:
Double-well potential curve
=> Strong anharmonicity
=> Exciton-phonon coupling ↑
Nat. Rev. Chem. 2021, 5, 838. JACS, 2016, 138, 11820. Phys. Rev. Lett. 2017, 118, 136001. JACS. 2022, 144, 27, 12247
([Xe]6s2)
([Ar])
Exciton-Phonon Coupling
Lattice Anharmonicity
Pb2+ 6s2 LPE
Notes: LPE enhances EPC.
Give Examples.

## Slide 7: 1.3 ns2 Lone Pair Effect (LPE)
Effects on Excited States
Ground State:
ns2 → (sp)2
LPE active
Excited State:
ns1np1 → (sp)1(sp*)1
LPE inactive
LPE enhances exciton-phonon coupling.
Notes: LPE changes excited state properties.
- vanish of LPE in excited state;
- Hot carriers relaxation(?)
- Coherent phonons (but no articles in this topic!)

## Slide 8: 1.4 Exciton-Phonon Coupling (EPC)
ACS Nano 2020, 14, 3, 3621. Acc. Chem. Res. 2018, 51, 3, 619. Nat. Comm. 2020, 11, 2035. ACS Nano 2019, 13, 11, 12621–12629
Emission Spectrum
Carrier
Self-Trapping
Exciton Transport
Excited State Dynamics
Notes: Researches on EPC tuning Photophysics, examples;
Change figure to F-C curves
What is EPC;
What photophysics does it influence (Examples)

## Slide 9: 1.5 Research Overview
ns2 Lone Pair
Effect
......
?
Photophysical Properties
Coherent Phonons
Exciton
Diffusivity
Light Emission
Influence?
Mechanism?
Structure-property Relationship?

## Slide 10: 1.5 Research Overview
Part. 1: Origin of ns2 LPE & tuning PLQY (Done)
- Large LA elongates Pb-I bond length and induces ns2 LPE;
- ns2 LPE enhances EPC and quenches PL;
Part. 2: ns2 LPE tuning exciton diffusivity (On-going)
- ns2 LPE enhances exciton scattering;
- Strong LPE will decrease exciton diffusivity (expected)
Part. 3: Excited-state properties upon ns2 LPE phase transition (Scheduled)
- Use coherent phonon spectrum to evaluate EPC upon LPE transition.

## Slide 11
Part. 2
Current Progress
LPE tuning structural distortion
LPE tuning PLQY
LPE tuning exciton diffusivity

## Slide 12: 2.1 Origin of ns2 LPE
LA Size
- Undersized LA --> Octahedral tilting
- Oversized LA ----> Pb off-centering
Off-centering Heterogeneity
R-MBA: in-plane off-centered
CHEA: out-of-plane off-centered
also validated in 18 other samples.
Angew. Chem. Int. Ed. 2023, 62, e202304515.
Veff = 97.7 A3
Undersized LA
Octahedral tilting
Veff = 101.0 A3
Medium LA
Tiniest distortion
Veff = 108.9 A3
Oversized LA
Pb2+ off-centering
Effective volume
[NI8]

## Slide 13: 2.1 Origin of ns2 LPE
DFT Calculation Results
Model: Cs2PbI4
Angew. Chem. Int. Ed. 2023, 62, e202304515.
Stretched Axis
Anharmonic Double-well
Unstretched Axis
Harmonic Parabola
Pb-I elongation induces 6s2 LPE
Notes: remove ELF
add stretch mode

## Slide 14: 2.2 Correlating ns2 LPE with PLQY
Urbach Tail & Asymmetry Factor (AF)
Both reflect the exciton-phonon coupling (EPC) strength;
Urbach tail: low-energy tailing of PL peak
EU: Urbach energy
Asymmetry Factor (AF):
An easier way to quantize EU.
Stronger EPC → Larger EU → Longer Tail
→ Larger AF
J. Phys. D: Appl. Phys. 2021, 54, 383001. Angew. Chem. Int. Ed. 2023, 62, e202304515.
(Weak EPC)
(Strong EPC)

## Slide 15: 2.2 Correlating ns2 LPE with PLQY
Angew. Chem. Int. Ed. 2023, 62, e202304515.
AF vs. Pb-I bond length
Relative PLQY vs. AF
Octahedral tilting 2D LHPs
(PA)2PbI4
(BA)2PbI4

## Slide 16: 2.2 Correlating ns2 LPE with PLQY
Shortening Pb-I bond Length by Pressure
As P increases:
- Pb-I bond length ↓;
- PL intensity ↑ then ↓;
- AF ↓;
- Raman peak frequency ↑;
- Raman central peak ↓;
All indicate less tendency of 6s2 LPE because of the shortening of Pb-I bond length.
Angew. Chem. Int. Ed. 2023, 62, e202304515.

## Slide 17: Details of this work are available online:

## Slide 18: 2.3 Measuring Exciton Diffusivity
Exciton Diffusion Dynamics
Classic diffusion model & PL:
solution:
or
Exciton concentration follows Gaussian shape .
Exciton diffusivity D is calculated from:
Nat. Comm. 2020, 11, 664. Adv. Energy Mater. 2020, 10, 1903781.

## Slide 19: 2.3 Measuring Exciton Diffusivity
Exciton Diffusivity of 2D LHPs
1. Rigidity dominates
4RAn series:
Rigid LA suppresses EPC, despite tilting
2. Distortion dominates
Tilting & ns2 LPE enhance EPC;
Exciton scattering ↑, diffusivity ↓
Unpublished
LA Cation | Structural Distortion Type | Diffusivity (cm2s-1)
4tFMPMA | Tilting | 4.730
4ClAn | Tilting | 2.174
4BrAn | Tilting | 1.458
4BuAn | Minor Tilting | 0.640
4FPEA | Intermediate | 0.613
PEA | Intermediate | 0.204
R-MBA | Off-center | 0.168
4DFCHA | Off-center | 0.020
PA | Tilting | 0.016
Rigidity dominating
EPC dominating

## Slide 20
Part. 3
Future Plan
Enhancing LPE in other systems
LPE tuning exciton diffusivity
LPE tuning excited-state properties

## Slide 21: 3.1 ns2 LPE in Other Halide Perovskites
n=1 2D LHP:
n>1 Quasi-2D LHP:
Introducing A cation
New dimension of tuning
Achieve higher ns2 LPE extent

## Slide 22: 3.1 ns2 LPE in Other Halide Perovskites
2D Sn/Ge Perovskites
ns2 LPE tendency: Pb2+ < Sn2+ < Ge2+
Stronger LPE, larger difference
Challenges
1. Oxidation
2. Lower PLQY
High LPE tendency, EPC ↑, PLQY ↓.
Low S/N ratio in some tests
JACS, 2022, 144, 18030.
Pb
Sn
Ge

## Slide 23: 3.2 Measuring Exciton Diffusivity
Instruments
Exciton Diffusivity
Data Analysis
LPE
Temperature
Excitation Power
Trap State

## Slide 24: 3.2 Measuring Exciton Diffusivity
New LA Series
Diffusivity ?

## Slide 25: 3.3 LPE-related Phase Transition
For double-well potential curve:
: Static LPE
: Dynamic LPE
Nat. Rev. Chem. 2021, 5, 838.
Notes: Remove irrelevant figs

## Slide 26: 3.3 LPE-related Phase Transition
Coherent Phonon Spectrum
Lattice vibration frequency:
Lattice vibration timescale ≈ detection timescale
Upon vibration:
- dielectric constant ;
- Refraction index ;
- Reflection ;
- Absorption ; ......
Phys. Rev. Mater. 2022, 6, 095401. J. Phys. Chem. Lett. 2022, 13, 4073.
Signal Oscillation
Coherent Phonon Frequency
Fourier Transformation
Time (ps)
Absorption Spectrum

## Slide 27
Acknowledgements
The Fu Lab 2023
Advisor: Dr. Yongping Fu
SCXRD refinement:
Xiaofan Jiang
Xinyu Li @ Fu Lab
Dr. Xiaotong Li @ Caltech
DFT calculations:
Yu Tao
Dr. Chen Li @ PKU
High-pressure PL, Raman, PXRD:
Tonghuan Fu
Dr. Songhao Guo
Prof. Xujie Lü @ HPSTAR
Microscope tech support:
Dr. Yan Guan @ PKU

## Slide 28
Thanks for your attention!

## Slide 29: 1.1 2D Halide Perovskites
Electronic Structure
Organic layer: HOMO - LUMO gap
Inorganic layer: VBM - CBM bandgap
In general, ==> Quantum Confinement
e- and h+ trapped in inorganic layer, forming exciton
In inorganic layer:
VBM: (B2+ ns + X np)*
CBM: (B2+ np + X ns&np)*
Inorganic lattice dominates the excitonic properties.
Chem. Rev. 2019, 119, 3140. JACS, 2019, 141, 1171.
VBM: (Pb ns + I np)*
CBM: (Pb np + I ns&np)*

## Slide 30: 1.1 2D Halide Perovskites
Tuning the Properties
.
LA+ chemical engineering
ns2 lone pair effect
Inorganic layer distortion
Exciton-phonon coupling
Emission wavelength
Carrier
mobility
PLQY
......

## Slide 31: 1.3 Exciton-Phonon Coupling (EPC)
How to Measure EPC Strength
J. Phys. Chem. Lett. 2022, 13, 4073.
Temperature-dependent Photoluminescence (TDPL)
Raman central peak
Transient absorption &
Coherent phonon spectrum

## Slide 32: 1.5 Exciton Diffusion
Nat. Comm. 2020, 11, 2035. Adv. Optical Mater. 2021, 9, 2001875
High-mobility semiconductor devices?
Lattice Rigidity
Energy Disorder
ns2 LPE?
?
Notes: to part 2 or:
add device importance

## Slide 33: 2.1 Structural Distortions in 2D LHP
ns2 LPE in 3D LHP
t < 1 Undersized A+ Octahedral tilting
t ≈ 1 Intermediate A+ Tiniest distortion
t > 1 Oversized A+ Pb2+ off-center displacement
JACS, 2022, 144, 12247.
Tolerance factor:

## Slide 34: 2.1 Structural Distortions in 2D LHP
ns2 LPE in 2D LHP
"2. Pb off-centering is orientational:
R-MBA: in-plane off-centered
CHEA: out-of-plane off-centered"
LPE is correlated with the Pb-I elongation direction;
R-MBA (108.9 A3) expands horizontal Pb-I;
=> in-plane expansion & off-centering
CHEA (99.5 A3) expands vertical Pb-I;
=> out-of-plane expansion & off-centering
Such correlation is valid across 18 other samples.
Angew. Chem. Int. Ed. 2023, 62, e202304515.
(R-MBA)2PbI4
in-plane expansion
(CHEA)2PbI4
out-of-plane expansion

## Slide 35: 2.2 Origin of ns2 LPE
Off-centering Vector
Octahedral Coordinates
X axis: in-plane longer
Y axis: in-plane shorter
Z axis: out-of-plane
Projected Off-centering Vector
Angew. Chem. Int. Ed. 2023, 62, e202304515.
Notes: delete

## Slide 36: 2.2 Electron Localization Function (ELF)

## Slide 37: 2.4 ns2 LPE and Exciton-Phonon Coupling
Raman Central Peak
Pb2+ hopping causes polar fluctuation
enhancing lattice anharmonicity & EPC
=> 0 cm-1, broadband background
Results:
Octahedral tilting ---- Strong central peak
Intermediate ---------- Weak central peak
ns2 LPE --------------- Strong central peak
Angew. Chem. Int. Ed. 2023, 62, e202304515.
Octahedral tilting
Intermediate
ns2 LPE /
Pb off-centering

## Slide 38: 2.4 ns2 LPE and Exciton-Phonon Coupling
Dynamic & Static Distortion
Nat. Rev. Chem. 2021, 5, 838. Angew. Chem. Int. Ed. 2023, 62, e202304515.

## Slide 39: 2.3 Measuring Exciton Diffusivity
Impact of Structural Distortion Type
We designed chemically similar LAs;
Diffusivity shows no trend due to trap-state emission.
Unpublished
LA Cation | Structural Distortion Type | Diffusivity (cm2s-1)
2MePEA | Tilting | 0.262 ± 0.087
3MePEA | Off-center | 0.303 ± 0.107
4MePEA | Intermediate | 0.174 ± 0.051

## Slide 40: 2.7 Impact of Trap States
Free & Trapped Exciton Diffusion
Free Exciton (FE) Trapped Exciton (TE)
(4BrAn)2PbI4 shows strong TE emission;
FE and TE emissions can be separated by filters;
FE diffusion:
- Narrow Voigt distribution;
- "Accelerating" diffusion;
TE diffusion:
- Broad irregular distribution;
- "Decelerating" diffusion;
Unpublished
FE
TE

## Slide 41: 2.8 Exciton Diffusion Dynamics
Different shapes of σ2-t curve
straight line
r-shape
J-shape
S-shape
reverse-S

## Slide 42: 3.4 Hypothesis of Trapped Exciton Diffusion
A possible model
1. There's a defect saturation level ;
2. FE traps fast, while TE detraps slow;
()
3. FE has shorter lifetime than TE;
()
FE
TE
Overall - normalized
FE
TE
Overall
Fluorescent Decay
Diffusion curve

## Slide 43: 3.4 Hypothesis of Trapped Exciton Diffusion
1. Excitation
2. Trapping
3. Transition
4. TE-dominating
5. TE-diffusion
FE diffusion
TE diffusion
Peak shape evolution